## Slide 1: SUPERCONDUCTIVITY and CRYOGENICS for accelerators
D. LONGUEVERGNE
04/06/2024

## Slide 2: OUTLINE
  Why superconductivity for acceleration ?
  Superconductivity : models and limitations
  Superconducting materials (properties and what they are good for)
  Cryogenics
  Operation of an accelerator (from perturbations to failures)
  Beam losses

## Slide 3: OUTLINE
  Why superconductivity for acceleration ?
    Magnets
    Accelerating Cavities
  Superconductivity : models and limitations
    History
    2 fluids model (London theory)
    Ginsburg-Landau theory
    Type of superconductors
    BCS theory (Bardeen Cooper Schrieffer)
  Superconducting materials (properties and what they are good for)

## Slide 4: WHY SUPERCONDUCTIVITY for ACCELERATION ?
In a particle accelerator, there are 2 types of major components :
    The focusing and bending components
    All along the acceleration, the particles have to be guided and focused (magnetic and electric fields).
    More information in course « beam transverse dynamics » (J. Michaud)
    Due to limitation of room temperature magnets (saturation of iron < 2T), superconducting technology is required especially for heavy particles and at very high energy.
    The accelerating components
    All accelerators use either a static or an oscillating electric field to accelerate.
    Room temperature RF technology is easier to build but shows many constraints because of power dissipations. Superconducting technology is compulsory for CW high current applications.

## Slide 5: WHY SUPERCONDUCTIVITY for MAGNETS ?
Superconducting magnet is required for high energy or high current applications
    Reduction of radius of curvature and power consumption
    With room temperature magnets, the LHC circumference would be 120 km and the power consumption impossible to handle
    Bigger beam pipe aperture as B  I0/aperture for dipole , I0/aperture2 for quadrupoles
    Bigger transverse acceptance
    Less beam losses, Less contraints for alignment.
http://www.lhc-closer.es/1/4/6/1

## Slide 6: WHY SUPERCONDUCTIVITY for MAGNETS ?

## Slide 7: WHY SUPERCONDUCTIVITY for ACCELERATION ?
Superconducting RF is compulsory for CW high-current operations :
for a given Vacc, NC, PRF  -1/2 , for SC, PRF  
Lower frequency  Larger longitudinal acceptance
Larger structure  Larger transverse acceptance
      Reduced beam losses
Energy efficiency is better : Pcryo + PRF-SC < PRF-NC
For SC cavities PRF-SC ~ 10 W (Qo ~ 5E9) @ 6.4 MV/m
To accelerate : PRF ~ 10W + Pbeam, Pcryo ~ (10W+10W)*500 ~ 10 kW => IN TOTAL : Plost ~ 10.01 kW
For NC cavities PRF-NC ~ 100 kW (Qo ~ 5e5) @ 6.4 MV/m
To accelerate : PRF-NC ~ 100 kW + Pbeam, Pcooling ~ 100 kW => IN TOTAL : Plost ~ 200 kW
Higher accelerating gradient achievable in CW
(in practice… not in theory) as PRF  Eacc2.
      Reduced linac length
  - If CW => low accelerating gradient
  (RFQ : Eacc ~ 0.3 MV/m, 100kW on 4m)
  - If High gradient => low duty cycle (< 10%)
NC = Normal conducting
SC = Superconducting
NLC, 11.4 GHz
Elliptical cavity, 1.3 GHz
NC
SC
1m

## Slide 8: WHY SUPERCONDUCTIVITY ?
    For NC cavities, power dissipation is the main constraint. Design is optimized to limit dissipations
    For SC cavities, power dissipation is less a constraint. Design is more free to optimize other parameters (acceptance, stability, …).
    BUT SC technology is a complementary solution because it has its own weaknesses :
        For magnets :
        Huge magnetic forces requires very stiff mechanical structures (training of magnets)
        Huge magnetic energy released if a quench happens (can quench if small displacement of wires of few microns!!)
        Very slow to ramp up or decrease field (magnetization)
        Need to be housed in a “cryomodule”  complex design
        Careful with energy deposition because of synchrotron radiation
        For cavities :
        Very sensitive (quench, Q-switch, surface resistance, trapped magnetic flux, Q-disease,…).
        More expensive (materials, larger structures)
        Need more time to mature a design as more complex
        Need to be housed in a “cryomodule”  complex design

## Slide 9: Superconductivity : history
  Some history :
    1868 : Discovery of Helium. Astronom Jules Janssen (France) noticed the yellow spectral emission lines of a new element in the chromosphere during a sun eclipse. Observed also in 1870 by J. N. Lockyer and named this new element from the sun : Helium as reference to the greek name of sun : “helios”.
    1877 : Oxygen (90K) and nitrogen (77K) liquified by Louis Cailletet (France) and Raoul Pictet (Switzerland)
    1893 : James Dewar invented the dewar vase.
    1895 : Helium is discovered on earth by sir W. Ramsay (England)
    1898 : Hydrogen (20K) liquified by Sir James (England)
    1908 : Kamerlingh Onnes liquified Helium
    1911 : Kamerlingh Onnes discovered superconductivity of mercury while studying the electrical behaviour of metals at low temperature.
    1933 : Walther Meissner discovered the Meissner effect : perfect diamagnetism
    1935 : “Two fluids model” by F. London
    1950 : Ginzburg-Landau theory
    1957 : BCS theory (Bardeen, Cooper and Schrieffer)
    1987 : Discovery of Y-Ba-Cu-O, first material with Tc > 77K

## Slide 10: Superconductivity : history
O. Gingras. "La supraconductivité non-conventionnelle du ruthénate de strontium: corrélations électroniques et couplage spin-orbite". Université de Montréal, Faculté des Arts et des Sciences. Montréal, Canada, 2022.

## Slide 11: Superconductivity : « the 2 fluids model »
  Phenomenological approach based on analogy with superfluidity (validity : T << Tc)
  Coexistence of normal and superconducting (“frictionless”) electrons N = ns(T)+ nn(T)
  2 fluids model   = n + is  solving the equation of propagation in a conducting material :
 | Normal conducting electron | Superconducting electron
Electronic density | Nn | Ns
Current-Electric field relation |  | 
For a sinusoidal electric field |  | 
Conductance |  | 
Maxwell équations

## Slide 12: Superconductivity : « the 2 fluids model »
  Surface resistance defined as Zs = Rs+i·Xs
  Interesting results : - Skin depth does not depend on frequency!
  - Rs is bigger for good conductors (metals)!
  This model does not explain existence of a critical magnetic field and its temperature dependence!
      To know the behaviour close to phase transition, we need another model
 | Normal conductor | Superconducting material (T<< Tc)
Electronic density | Nn | N=Nn+Ns with Nn << Ns
Skin depth |  | 
Surface resistance |  | 

## Slide 13: Superconductivity : Ginzburg-Landau theory
  Phenomenological approach based on second order phase transition of free energy
  Validity : for T ~ Tc
  The superconducting state is stable
   Its free energy is lower than the normal state.
  Superconductivity can be broken by magnetic field
   Critical magnetic Hc can be defined
  Complex superconducting order parameter is defined by :
  For T  Tc,  is small, the free energy can be expanded in a taylor series :
  With 0, m* and β are phenomenological parameters >0, Tc is the temperature of phase transition.
  Here appears that temperature and magnetic field impact directly the difference of free energy and thus the stability of the superconducting phase.
With

## Slide 14: Superconductivity : Ginzburg-Landau theory
  If we assume no magnetic field, the equation simplifies as :
  If (T)>0  T>Tc  Fs>Fn, superconducting phase cannot exist as  can only be 0
  If (T)<0  T<Tc  Fs<Fn, superconducting phase can exist as   0
              For T~ Tc,
              Very close to the empirical formula
              Ginzburg-Landau equations predicted 2 new parameters :
                Penetration depth of magnetic field
                Coherence length : ~ penetration depth of superconductivity

## Slide 15: Superconductivity : Type of superconductors
  A parameter , independent of temperature, can be defined as the ratio between  and 
  For 0< <1/2, normal and superconducting phase can’t coexist in the material TYPE I
             Meissner effect is total
  For > 1/2, normal and superconducting phase can coexist (energetically favorable) above a field Hc1 in the material TYPE II  Meissner effect is partial
Hc

## Slide 16: Superconductivity : Type of superconductors
  Solving Ginzburg-Landau equations shows that the normal zones are cylindrical and are called vortices with a elementary magnetic flux

## Slide 17: Superconductivity : BCS THEORY
  Theory based on quantum mechanics made up by Bardeen, Cooper and Schrieffer (1957)
  Superconductivity comes from the interactions between conduction electrons and vibrations of atoms (phonons).
  Nothing to do with nature of atoms but with their arrangements (crystal structure)
  An electron creates a positive screening cloud around itself (attraction of positive ions of the lattice) that creates an attractive force for another electron
      2 electrons are paired : Cooper pair (opposite spin and momentum)
  To break a Cooper pair, a finite energy of is required
  The bigger the normal resistivity, the bigger the electron-phonon interaction, the bigger the pairing energy.
Normal conductor
Superconductor
2

## Slide 18: Superconductivity : BCS THEORY
2
  BCS theory predicted the following formula for the surface resistance of a superconductor :
  Depend on material properties.
  Depend on temperature (probability of a Cooper pair to be broken by thermal agitation)
  To be compared to London formula :

## Slide 19: Superconducting materials : what is used today ?
Material | Hc (mT) | Hc1(mT) | Hc2 (T) | Tc (K)
Sn | 31 | / | / | 3.72
Hg | 41 | / | / | 4.15
Pb | 80 | / | / | 7.2
Nb | 200 | 170 | 0.4 | 9.2
NbTi | ? | 10 | 15 | 10
Nb3Sn | 540 | 50 | 30 | 18
MgB2 | 430 | 30 | 3.5 | 40
NbN | 230 | 20 | 15 | 16.2
YBaCuO | 1400 | 10 | 100 | 93
Best for cavities (Bc1 matters)
Best for magnets (Bc2 matters)

## Slide 20: Superconducting materials
  Cavities :
    Best material : Bulk Niobium : mechanical and physical properties
    are optimal. Metal => high formability and workability.
    New materials : MgB2, Nb3Sn, … alloys can’t be worked easily
    => thin layer deposition on Niobium or multilayer (SIS).
  Magnets :
    Rutherford cable : NbTi filaments embedded in a copper matrix
    Heat and current extraction. Example : LHC magnets :
    New material : Nb3Sn to achieve 15 T but very brittle!
  http://lhc-machine-outreach.web.cern.ch/components/cable.htm
In LHC :
1200 magnets
7600 km of cable
36 strands per cable
6400 filaments per strands
Total length of filaments
10 times the distance between earth and sun !!!
0.825 mm
6 um

## Slide 21: OUTLINE
  Cryogenics
    What’s the right temperature of operation?
    Cryostats and interfaces
  Operation of an accelerator (from perturbations to failures)
    Perturbation during operation (focus on accelerating cavities)
    Failures during operation
    Beam losses

## Slide 22: CRYOGENICS ( what’s the right T° ?)
    Superconductivity requires to operate cavities (Nb) and magnets (NbTi) below 9.2K and 10K : only liquid helium at 4.2 K :
    BUT :
      Very low latent heat of vaporization and very expensive to liquefy (> 25 €/L today from a company)
      Critical field depend on temperature :
       Hc(4.2K) = 0.8H0
      Surface resistance depend on frequency and temperature :
      Power dissipation is limited by heat
      exchange coefficient :
      high power dissipations may require to
      operate with superfluid helium < 2K.
Element | Tliq (K)
Helium | 4.2
Hydrogen | 20.4
Neon | 27.1
Nitrogen | 77.4
Oxygen | 90.2
RBCS (n) | 4.2K | 2.2K | 2K | 1.8K | 1.5K
1300 MHz | 600 | 33 | 15 | 6.5 | 1.2
700 MHz | 174 | 9.5 | 4.3 | 1.9 | 0.35
352 MHz | 44 | 2.5 | 1 | 0.48 | 0.09
88 MHz | 3 | 0.15 | 0.07 | 0.03 | 0.006

## Slide 23: CRYOGENICS
Normal helium
Superfluid helium
S. W. Van Sciver, “Helium cryogenics”, Plenum press, 1986
~100 W/m2/K
~ 5000 W/m2/K

## Slide 24: OUTLINE
  Cryogenics
    What’s the right temperature of operation?
    Cryostats and interfaces
  Operation of an accelerator (from perturbations to failures)
    Perturbation during operation (focus on accelerating cavities)
    Failures during operation
    Beam losses

## Slide 25: MAIN COMPONENTS in a CRYOMODULE
ESS Spoke Cryomodule
Vacuum vessel
Thermal shield
Cryogenic piping (supply and exhaust)
Magnetic
shield
Superconducting cavity
Vacuum vessel
  Interface (valves, beam pipe)
  Thermal Insulation
  Limiting convection losses
Supporting components : support + alignment
MAIN COMPONENTS
Supporting components
  Supporting and positioning
  the cold mass
  Limiting conduction losses
Thermal shields
  Thermal Insulation (80K)
  Limiting radiation losses
Cryogenic piping
  Cryogenic environment
  Ensuring supply of Lhe and
  degassing of GHe
Magnetic shield
  Reduction of earth
  magnetic field
Cold mass (cavities, magnets)
Beam
Frequency tuning system
RF power coupler
300K
2K

## Slide 26: CRYOGENICS (thermal insulation)
300K vacuum tank
50-80K shield
+ MLI (30 layers)
Mechanical support
Beam tube
1.5-4K cold mass
+ MLI (10 layers)
Current leads
Power coupler
Piping, wiring
Conduction
Radiation
Heat sink

## Slide 27: CRYOGENICS
        Superconducting structures cooled by helium have to be isolated in “cryomodules” :
    Limit heat losses by reducing :
      Conduction : ↑ thermal resistivity (material), ↓ surface area, ↑ length , liquid nitrogen heat sinks.
      Convection : under vacuum
      Radiation : liquid nitrogen shield, multi-layer insulation (MLI) : multiple high reflective foils (aluminized mylar) separated by low conduction spacer (bridal veil)
     Do not disturb magnet or cavity operation :
      Thermal stability : constant and homogeneous temperature of cavity or magnet even with power losses.
      Interfaces : RF and electrical feedthrough, instrumentation.
      Mechanical stability : keep alignment although thermal contractions, pressure forces, low mechanical vibration transmission.

## Slide 28: CRYOGENICS ( high energy cryomodules)
XFEL
LHC
GRP
Cavity
70K shield
4K shield
Vacuum vessel
Coupler port
Support post
2 phase
pipe
Sliding support
Invar rod
XFEL

## Slide 29: CRYOGENICS ( low energy cryomodules)
https://frib.msu.edu/
FRIB Cryomodule
ISAC2 cryomodule @ TRIUMF

## Slide 30: VACUUM VESSEL
ESS Spoke Cryomodule:
1,3m
2,8m
SPL Short test Cryomodule:
~ 7m
0,8m
SPIRAL2 Cryomodule B:
2,8m
1,16m
Examples of vacuum vessel studied at IJCLab:
MAIN COMPONENTS

## Slide 31: CRYOGENICS :Superconducting magnets
DIPOLES
QUADRIPOLES
SOLENOID+BUCKLING COILS

## Slide 32: CRYOGENICS :Superconducting cavities
RBCS (nΩ) | 4.2K | 2K | 1.5K
1300 MHz | 600 | 15 | 1.2
700 MHz | 174 | 4.3 | 0.35
352 MHz | 44 | 1 | 9E-2
88 MHz | 3 | 7E-2 | 6E-3
ESS β=0.67, 700 MHz
XFEL β= 1, 1.3 GHz
ESS β=0.5, 352 MHz
MYRRHA β=0.37, 352 MHz
2K
SPIRAL2, β=0.12, 88 MHz
SARAF β=0.091, 176MHz
β=0.181, 176MHz
IAP β=0.07, 215MHz
4K
  Particle velocity (β)  Cavity frequency (Fo)
β
1
0.65
0.3
0.03
Elliptical cavity (700-3000 MHz)
Quarter-Wave resonators
(80-150 MHz)
Half-wave resonator (150-400 MHz)
0.15
CH resonator
(200-350 MHz)

## Slide 33: Operation of an accelerator (from perturbations to failures)
    Perturbation during operation (focus on accelerating cavities)
      Frequency perturbations (microphonics, Lorentz detuning)
      Multipacting
      Field emission
      Quench
    Failures during operation
      Type of failures
      Statistics
    Beam losses

## Slide 34: PERTURBATIONS : frequency perturbations
  The frequency of RF cavities have to be
  exactly synchronized to beam frequency
  (bunched beam, see longitudinal beam
  dynamics).
   Master oscillator.
  RF power is generated at fixed frequency
  But cavity is a resonator (second order filter)
  with a resonance frequency F0 subject to perturbations.
   F0 has to be tuned permanently to match RF frequency
amplitude
phase
Additional RF power required versus cavity detuning

## Slide 35: Example of frequency tuner system
Piezo-electric actuators
Stepping motor

## Slide 36: PERTURBATIONS : frequency perturbations
  RF regulation loop to compensate several type of frequency perturbations :
      Static or very slow perturbations : fabrication errors, thermal contraction, pressure forces, Lorentz forces (CW), …
       Compensated by frequency tuning system (motor)
      Dynamic perturbations : mechanical resonance (microphonics), Lorentz forces (pulsed operation), …
       Compensated by frequency tuning system (piezo) and RF regulation loop (LLRF)
Vibration sources | area | Frequency range
Primary pumping system | Close to cryostat | 50 Hz
Turbo pump | Close to cryostat | kHz
Valves / motors | Cryostat | pulse
Helium boiling | Cavity | Depends on dissipations
Lorentz forces (pulsed) | cavity | RF pulse
Human activity | Environment | Tens of Hz

## Slide 37: PERTURBATIONS : frequency perturbations
67 Hz
230 Hz
355 Hz
420 Hz
480 Hz
  Microphonics : resonance frequency perturbations caused by mechanical resonance of cavity
Example of mechanical resonance of quarter wave resonator for Spiral2
Frequency detuning (Hz)
Mechanical frequency (Hz)

## Slide 38: PERTURBATIONS : frequency perturbations
  Lorentz forces : Mechanical deformation caused by electromagnetic pressure radiation
Example of lorentz forces on 1-cell elliptical cavity

## Slide 39: PERTURBATIONS : Multipacting
  Multiplication of electrons in resonance with RF field
  RF power goes into electron avalanche instead of charging up the cavity
  Requirements to meet resonance conditions
      Geometry
      Field distribution
      Coefficient of secondary electron emission

## Slide 40: PERTURBATIONS : Multipacting
  Observed as a “barrier” when Q0 versus accelerating gradient is plotted.
  Can be processed with time by increasing RF power.
Accelerating gradient (MV/m)
Spiral2 cavity
Eacc = 0,103 MV/m
Eacc = 1,3 MV/m

## Slide 41: PERTURBATIONS : Field emission
  Electrons are extracted from the surface by the electric field (tunnel effect).
  For a perfect flat surface, no emission up to few GV/m
  But because of surface defects, pollution  Enhancement of electric field
  Electron emission is thus possible as low as few MV/m.
  The electron current follows the Fowler & Nordheim
  quantum theory

## Slide 42: PERTURBATIONS : field emission
  Observed as a rapid decrease of the Q0 versus accelerating gradient.
  What are the induced limitations :
      X-rays emission by brehmsstrahlung : safety problems
      Local heating can provoke early quench
      Additional dissipation in helium bath
  Can be avoided by extensive cleaning of cavity (High pressure rinsing, clean room assembly)
  Can be processed by simple increasing RF power or by injecting He gas to favor emission
Spiral2 cavity

## Slide 43: PERTURBATIONS : quench
  Superconducting properties are lost because of :
        A too high magnetic field (Hc1 for cavities, Hc2 for magnets)
        A too high temperature
        A too high current density
  Quench can happen at lower magnetic field or temperature than theoritical one because of
        Surface defect : local enhancement of magnetic field
        Surface pollution : local heating (field emission, resistive defect, vortices…)
        Filament motion under magnetic forces
  Structures (cavity or magnet) can be “trained” to push away the quench if possible
        For cavities not so dangerous as no energy is stored but careful in case of high current beams
        For magnets, the quench can be really destructive

## Slide 44: accident : example LHC in 2008
  A superconducting wire had a defect and quenched.
  Electrical arc punctured helium circuit and degraded isolation vacuum  helium boiled off quickly and huge pressure wave destroyed about 30 magnets
Courtesy of R. Schmidt, CERN

## Slide 45: Failures during operation
  Several type of failures : operation error, equipment failure, external (electrical supply), experiments
  And at different stages of acceleration :
        At low energy, minor damages as beam power and stored energy is low.
        At high energy, minor damages if protection system is fast enough
              severe damages if protection too slow, not well dimensioned or inexistent
Machine protection system shut off beam in less than 30 µs
Spallation Neutron Source, Oak Ridge

## Slide 46: Failures during operation : LHC example

## Slide 47: BEAM LOSSES
  Continuous beam losses :
  Due to residual gas stripping, intra-beam stripping, misalignment of components, beam shaping and handling (collimation, chicane, chopper, …)
        Safety problems (activation), maintenance delays, slow pollution in RF cavities, …
        Reduced with beam cleaning (collimation), bigger apertures, CW operations (compared to pulsed operations), components adjustment, …
        1W/m is usually the upper limit.
Courtesy of J. L. Biarrotte

## Slide 48: BEAM losses : examples
  Occasional beam losses (accident):
  RF or magnetic regulation loop perturbations, ion source fluctuations, interlocks, cavity or magnet failure, …
        Can cause severe damages with high power beams (beam tube melting, leak, pollution, explosion, …)

## Slide 49: BEAM losses : examples
Spiral2 (GANIL) :
200 kW (CW)
SNS (Spallation Neutron Source, USA) :
1 MW (average)
ESS (European Spallation Source, Sweden):
5 MW (average)
LHC (Large Hadron Collider) :
4 TW (average)

## Slide 50: BEAM losses : example LHC
Energy stored in LHC beam : 360 MJ enough to melt 5.6 tons of gold
  Beam losses have to be maintained very low
  In case of excessive beam losses, detection has to happen very quickly and beam has to be dumped immediately
9 GJ stored in dipole magnets enough to melt 45 tons of gold.
Courtesy of R. Schmidt, CERN

## Slide 51: HOPE YOU ENJOYED KNOWING MORE ABOUT SUPERCONDUCTIVITY AND CRYOGENICS FOR ACCELERATORS
THE END

## Slide 52: Example of 120°C baking : SPIRAL2 QWR @ IPNO
After 72h drying  48 h baking @ 120°C
“Forced” air flow inside the helium vessel + heater on the cavity bottom
Cavity wrapped in a foil blanket
Heater (not shown) glued onto the copper cap
Input
~120°C
Output
~110°C
Heater
~110°C

## Slide 53: The MYRRHA spoke cryomodule (6)

## Slide 54: PERTURBATIONS : Q-disease or 100K effect
  When a cavity was cooled down or warmed up too slowly, the quality factor (i.e power dissipation) could fall of one order of magnitude.
  The hydrogen trapped in Niobium precipitates in an ordered phase (β), which shows no superconducting properties  surface resistance is degraded
  Hydrogen sources : surface treatment (chemical etching), residual gas in atmosphere.
  If fast cool down, no time to precipitate (<1h between 150K-50K)
  Solution to avoid Q-disease : high temperature degassing at 600°C during 6h.
        but expensive and time consuming.
Spiral2 cavity

## Slide 57: Superconductivity : history
From « The rise of the Superconductors », P.J. Ford, G.A. Saunders, CRC Press, 2005

## Slide 58: Example : cryogenic piping of a cryomodule

## Slide 59
Temperature field in an assembly  Thermal contractions and stresses
After the cool down, the temperature field in a cryomodule:
 Theses contractions can create some high thermal stresses.
Solving problem of stresses will depend on the type of connection between the components according to their function:
String of cavities at 2/4K: niobium, titanium, stainless steel...
Thermal shields at 50/80K: copper, aluminium
Cryogenic lines from 2K to 300K: stainless steel, aluminium...
Supports from 2K to 300K
String of cavities
Thermal shield
2-4K
50-80K
300K
- Supporting,
- Transferring cryo fluid
- Vacuum circuit
Thermal contractions and stresses
MECHANICAL ASPECTS
 Some thermal contractions appear on all components:
With different temperatures
With different materials

## Slide 60: CRYOGENICS (thermal contractions)
Fixed Point
Table Slider
Invar Rods
Cavity Sliders
DX : 3,5 mm
DX : 0.4 mm
DX : 0.1 mm
DZ
DZ
Mobile Point
LHC : total thermal contractions are 80m over the 27 km.

## Slide 61: CRYOGENICS :Superconducting cavities
Power coupler
Helium tank
SPOKE
CAVITY
ELLIPTICAL
CAVITY
Frequency tuning system